A Fundamental Shift in Water Disinfection – Research Into An Innovative UV LED Design

Jennifer G. Pagan1 , Oliver Lawal2, Paolo Batoni1

- Dot Metrics Technologies, 9201 University City Blvd, Grigg Hall, Charlotte, NC 28223, USA

- Aquionics Inc., 21 Kenton Lands Road, Erlanger, KY 41018, USA

Currently UV treatment of fluids is almost exclusively carried using Low and Medium Pressure lamp technology that incorporate mercury as a generation source for UV photons.  While UV treatment is replacing traditional chemical treatment in many applications, it still has a number of drawbacks.  UV light-emitting diodes (UV-LEDs) provide solutions to most of these drawbacks.

UV-C LEDs which emit radiation in the germicidal wavelengths (200 nm-300 nm) are an emerging technology with few manufacturers worldwide.  Commercial adoption of UV-C LEDs is impeded by extremely low external quantum efficiencies, typically below 3%.  However, despite their inefficiency, UV-C LEDs continue to generate interest for use in water disinfection applications.  Low optical output powers of UV-C LEDs necessitate the use of multichip packages to generate the power levels necessary to achieve disinfection.  High device thermals and UV emission combine to make multi-chip packages challenging and require the development of packaging materials which would provide lower thermal resistance and UV stability than those currently used in eh high brightness (HB) LED market.

Data taken from 265 nm LED from Sensor Electronic Technology (Columbia, SC) show that a 30 degree C jump in ambient temperature results in a more than 43% drop in peak output power.  This indicates, as is the case with visible LEDs, that the cooling of a UV-C LED is essential to maintaining optical output power levels.  In addition, testing of 254 nm TO-39 packaged LEDs demonstrated that when the LEDs are convectively (fan) cooled with a heat sink, the package temperature drops by 20 degree C.  The operating lifetime of the cooled LEDs was significantly increased over the as-packaged devices, indicating that optimized thermal management would have a significant impact on UV-C LED device performance.

Multi-chip packages which are necessary to achieve power levels adequate for disinfection exacerbate the heating issues.  While a single LED in a TO-39 header maintain around a 41 degree C temperature, the same package with 8 dice exceeded 111 degree C (the IR camera maximum).

In addition to output power concerns, there are technological roadblocks to understanding how to incorporate UV-C LEDs into mercury heritage applications such as water disinfection.  The inherent benefits of UV-C LEDs, which are; mercury free, instant on/off, low voltage sources, create key drivers for market adoption.

In addition, recent results show that a UV-C LED treatment device can effectively disinfect up to 12 gpm/watt of water, compared to less than 1 gpm/watt for a conventional mercury lamp based system.  On the cusp of such a paradigm shift, a comprehensive understanding of UV-C LEDs from both a technological and biological standpoint will be critical to implementing the technology into disinfection and sterilization systems.

Keywords:  UV Light-Emitting Diodes, Water, Disinfection, Sterilization