FluMET: Cerium Based Adsorber

- Reactions for Fluoride ion is adsorption

- Cerium based adsorber resin can be flexible use for volume ranges

- pH and Redox substances need controlling with pre-treatment

- Adsorbs Fluoride ions under the level 1 mg/liter

- Annual replacement 10% of volume

- Adsorbed Fluoride can be removed from filter by regeneration. Allowing for smaller filter and cheaper running cost.

- The active component of the adsorber is a mixture of Ce(OH)4 + CeO2 x nH2O

- The active component is supported by an EVOH (ethylene vinyl-alcohol copolymer resin)  framework. EVOH is a food grade resin with the following structure:

- Adsorption capacity:

  - Dependent on the Fluoride concentration and the pH of the input water

  - Maximal fluoride concentration is 30 mg/liter

  - pH is optimal between 3 and 3.5

  - Equilibrium capacity: Maximum amount of Fluoride adsorbed in a liter of resin

- Saturation

  - The measured fluoride content of the filtered water follow a saturation curve

  - For a number of days depending on the actual capacity the output fluoride level will be close to 0 mg/l

Regeneration I.

Regeneration II.